






	ULTRA Q7 ANTIWEAR HYDRAULIC OIL
                                                                               32, 46, 68, 

	PERFORMANCE PROFILE
	

	DIN 51524 Part II
	
	

	APPLICATION

	A top quality oil with high degree of wear protection designed with highly refined base stocks and well balanced additive package. Recommended for high pressure hydraulic systems used in all mobile and stationary equipments operating under severe working conditions. Also used for circulation system, compressor pump, bearing and gear lubrication where recommended.

	KEY FEATURES

	· Extended oil life
· Enhanced thermal and hydrolytic stability 
· Excellent demulsibility power and air release capability
· Outstanding filterability and good shear stability
· Exceptional resistance to foaming and oxidation
· Good resistance to wear, corrosion and rust.
· Good compatibility with seals and soft metals
· Good friction characteristics resulting in lower running temperature


	TECHNICAL DATA

	CHARACTERISTICS
	TEST METHOD
	TYPICAL VALUE

	
	
	32
	46
	68

	Density at 15 oC, Kg/L
	ASTM D1298
	0.875
	0.880
	0.882

	Viscosity at 40 oC, cSt
	ASTM D445
	32
	46
	68

	Viscosity at 100 oC, cSt
	ASTM D445
	5.4
	6.8
	8.8

	Viscosity Index
	ASTM D2270
	102
	102
	102

	Flash Point, COC,  oC
	ASTM D92
	220
	220
	230

	Pour Point,  oC
	ASTM D97
	-18
	-18
	-18



